INSTALLATION METHOD FOR STAIR TREAD & NOSING

Preparation

Surfaces to which the stair tread or nosing is to be bonded must be clean, dry and free from grease.  This is achieved by thoroughly cleaning the substrate with “Recochem Premium All Purpose Thinners” and / or Isopropyl Alcohol.

Fixing Method

The recommended adhesive to be applied is ‘205 brush contact adhesive’, manufactured by TAC Adhesives Pty Ltd, 1-3 Tarnard Drive Braeside; although most other contact adhesives would be suitable (e.g. Nortons, available from Bunnings Hardware).  Please read directions thoroughly before use.

For surfaces that are porous such as concrete etc, it may be necessary to apply a sealer prior to bonding the stair tread.  Recommended procedure is to cover both the substrate and the nosing with a thin layer of contact adhesive using a brush.

Allow the adhesive to evaporate until it is no longer tacky to the touch.  This may take 5-15 minutes depending on the prevailing temperature and humidity.  Do not use below 10°C as condensed water may form on the adhesive film and prevent bonding.

Position one end of the nosing on the step and working from one edge, press firmly together.  Secure bond by running a roller over the surface or else by hammering the surface from the centre outwards to the ends using a padded block.

Clean up excess adhesive with Recochem All-Purpose thinners or mineral turpentine.

To remove extreme scuffing wipe occasionally or as required with low odour kerosene.

Cleaning Advice:

The Eva Stair Nosing and stair insert products are easily cleaned utilising standard cleaning procedures methods. To remove extreme scuffing the products should be wiped or mopped using odourless Kerosene. Odourless Kerosene will remove any rubber scuffing without scrubbing and without harming the EVA plastic Compound.